# Text boxes

Victory Lighting

Product Data Specification

Product Code: 64242520

Issue No: 7

Issue Date: 19 January 2007

| A | 900±2 | E |  |
| --- | --- | --- | --- |
| B |  | F | 10.5 |
| C | 230±5 | G | 836 nom |
| D |  | H | 5 max |

All dimensions in mm unless otherwise stated

- Use pumped lamp 2402500E886

- Cap: ceramic part 1 (Cap to be cemented). Code no: 206195

- Lead: single insulated with fork terminal. Code no: 205264

- Lamp to be dunched

- Crop length 896

| Volts | 240 | Colour Temp | 1950 |
| --- | --- | --- | --- |
| Watts | 2500 | Life | 5000 |
| Lumen/Watt | 1-2 | Burning Position | Universal |
| Finish | Clear | Leads | Single ins |
| Cap | Sk15 |  |  |

Authorised By

240v 2500w IR Lamp

(  Property of Victory Lighting Limited, Quay West, Salamander Quay, Harefield, Uxbridge, Middlesex. UB9 6NZ

Dimensions

Technical Data